## Slide 1: Rubber: Science, Technology and Applications
Dr. Naveen Kumar Sharma
Assistant Professor

## Slide 2: Introduction
Rubber is a natural or synthetic elastomer.
Highly elastic
Widely used in engineering and healthcare
Rubber is an elastic polymer made from natural plant latex or artificial petrochemicals. It stretches easily, bounces back to its original shape, resists water, and blocks electricity. People use it worldwide to make tires, seals, gloves, and hoses.
Types of Rubber
Natural Rubber: Harvested as a milky sap mostly from the Hevea brasiliensis tree.
Synthetic Rubber: Man-made in factories using petroleum byproducts (such as neoprene and SBR).
Key History and Processing
Ancient Roots: Indigenous groups in Mesoamerica first used plant latex to make waterproof cloth and balls.
The Name: Joseph Priestley found that the material could rub away pencil marks, which gave it the name "rubber".
Vulcanization: Invented in 1839, this heating process adds sulfur to make rubber strong, durable, and temperature-stable.

## Slide 3: History
Traditional latex use Mainly obtained from plant Heavea Brasiliensis ,18 39 Goodyear vulcanization, Synthetic rubber in 20th century
Olmecs and Mayans: Indigenous groups in Central and South America harvested latex sap from Hevea trees as early as 1600 BC.
Early Uses: They mixed the sap with plant juices to create bouncy balls for sacred games, waterproof shoes, and coated fabrics.
European Contact: Christopher Columbus and other explorers witnessed these waterproof items during voyages to the New World in the late 15th century.
The Industrial Breakthrough
Vulcanization (1839): American inventor Charles Goodyear accidentally dropped a mixture of rubber and sulfur onto a hot stove, discovering that the process stabilized the material into a durable, weather-resistant substance.
The Rubber Boom: The late 19th-century invention of pneumatic tires and automobiles sent global demand soaring, transforming Amazonian cities like Manaus into temporary centers of immense wealth.
Global Plantations: Seeds smuggled from Brazil to Southeast Asia successfully shifted raw production to massive managed plantations.
Synthetic Era
World War II: Wartime supply shortages cut off access to natural rubber plantations, driving intense research into petroleum-based alternatives.
Modern Markets: Synthetic rubber was heavily engineered and eventually matched or exceeded natural rubber production totals, supplying the majority of global needs today.

## Slide 4: Sources
Natural: Hevea brasiliensis, The tree Hevea Brasiliensis, which thrives at altitudes near 300m, high rainfall, and temperatures of 25–35°C.
Synthetic: SBR, NBR, Neoprene, Butyl, Silicone
Tapping: A precise surgical slice (~1 mm thick, 6 mm deep) is cut into the bark at a 30° angle to harvest fresh field latex.Field Latex Composition: Typically 30–35% rubber hydrocarbon, 60–65% water, alongside small fractions of proteins, resins, and ash.

## Slide 5: Structure
Natural rubber = cis-1,4-polyisoprene (C5H8)n

## Slide 6: Properties
Elasticity, tensile strength, insulation, abrasion resistance
Elasticity: Governed by molecular thermodynamics. Unstretched chains have high conformational entropy, reverting to disorder when released.Glass Transition (\(T_{g}\)): Around -70°C, molecular motion stops, causing the elastomer to transform into a brittle, glassy state.Strain-Induced Crystallization: Under tension, highly uniform cis-polyisoprene chains line up, forming crystal-like structures that inherently reinforce the material.

## Slide 7: Types
Natural vs Synthetic rubber
iscosity Stabilized (CV/LV): Treated with hydroxylamine hydrogen chloride to prevent storage hardening.Superior Processing (SP): Blend of vulcanized and unvulcanized latex that minimizes dimensional swell during extrusion.Thermoplastic NR (TPNR): A physical blend of natural rubber and polypropylene acting as a recyclable elastomer.Epoxidised NR (ENR): Chemically modified with peracids to introduce polar oxirane rings, boosting oil resistance and wet traction.

## Slide 8: Synthetic Rubbers
SBR, NBR, Neoprene, Butyl, Silicone

## Slide 9: Manufacturing
Latex→Coagulation→Rolling→Drying→Finished sheets
Spontaneous Coagulation: Bacteria ferment natural sugars into volatile fatty acids, causing field latex to destabilize and coagulate within 8–24 hours if untreated.Preservation: Ammonia or sodium sulphite is added to act as a bactericide and preserve stability.Controlled Coagulation: Dilute formic or acetic acid is added to lower the pH to 4.8, destabilizing the colloid into a manageable rubber slab.

## Slide 10: Vulcanization
Sulfur crosslinking improves strength and durability
Sulphur Curing: Accelerated sulphur networks create three main cross-link variations:Polysulphidics (\(S_{x}\)): Flexible, high tensile strengths, but poor thermal stability.
Monosulphidics (\(S_{1}\)): Thermally stable cross-links that yield outstanding heat aging behavior.
Efficient Vulcanisation (EV): High accelerator-to-sulphur ratios favor monosulphidic networks for heat-resistant applications.Non-Sulphur Peroxide Curing: Forms direct carbon-carbon bonds (\(C-C\)), providing unparalleled high-temperature stability.
Styrene-Butadiene Rubber (SBR): The most widespread general-purpose synthetic rubber, containing roughly 23% styrene.Lacks strain-induced crystallization, requiring reinforcing fillers (carbon black) for strong physical properties.
Polybutadiene Rubber (BR): Known for very high resilience and low heat build-up. Blended with NR/SBR to improve tire tread wear.
Polyisoprene Rubber (IR): The synthetic analog to natural rubber with high cis-content, offering better processing flow and lower ash content.

## Slide 11: Special-Purpose Synthetic Rubbers
Nitrile Rubber (NBR): Copolymer of butadiene and acrylonitrile. Highly polar nitrile groups grant exceptional oil and fuel swelling resistance.
Butyl Rubber (IIR): Copolymer of isobutylene with minimal isoprene. Possesses ultra-low gas permeability, making it perfect for inner liners and tubes.
Ethylene-Propylene-Diene (EPDM): Saturated hydrocarbon backbone with unsaturated side-chains. Resistant to ozone, weathering, and heat aging.
Chloroprene Rubber (CR / Neoprene): Displays excellent mechanical toughness along with flame, oil, and atmospheric weathering resistance.

## Slide 12: Compounding
Sulfur, ZnO, accelerators, carbon black, antioxidants
Why Compound? Raw rubber is physically weak, highly sensitive to temperature changes, and degrades rapidly in environmental air.Essential Ingredients:Peptizers: Chemical plasticizers that break down long polymer chains during mastication.
Vulcanising Systems: Cross-linking packages that tie chains together.
Fillers: Reinforcing agents (like Carbon Black) or non-reinforcing diluents.
Antidegradants: Antioxidants and antiozonants added to prolong operational service life.

## Slide 13
Key Ingredients in Rubber Formulations
Base Polymers: Natural rubber or synthetic options like SBR and EPDM provide the basic elastic framework.
Fillers: Reinforcing agents like carbon black or silica enhance strength, hardness, and wear resistance.
Plasticizers: Process oils or petroleum derivatives soften the mixture and improve flow during manufacturing.
Protective Agents: Antioxidants and antiozonants prevent degradation from heat, oxygen, and weather.
Curing Systems: Sulfur or peroxides create cross-links between polymer chains during vulcanization to lock in permanent elasticity and durability.

## Slide 14
The Compounding and Mixing Process
Mastication: Raw rubber is mechanically softened on an open mill or internal mixer to make it receptive to other chemicals.
Blending: Fillers, oils, and protective agents are systematically blended into the softened rubber base until uniform.
Curing Addition: Vulcanizing agents and accelerators are added near the end of mixing at controlled lower temperatures to prevent premature scorching or curing.
Shaping and Vulcanization: The mixed compound is shaped and heated, triggering chemical cross-linking that transforms the viscous mass into a resilient, elastic solid.

## Slide 15: Processing
Mixing→Mastication→Compounding→Shaping→Curing
Visual Grading (The Green Book): Classifies sheets by physical inspection of dirt, blemishes, rust, and molds (e.g., Ribbed Smoked Sheet RSS 1-6, Pale Crepe).
Technical Specification (TSR): Introduced in 1965 to eliminate visual grading subjectivities.
Key Tested Parameters:
  Dirt content (bark fragments and sand particles).
  Ash content (inorganic tracer residues).
  Nitrogen content (protein indicators driving creep behavior).
  Plasticity Retention Index (PRI) (oxidative degradation resistance).

## Slide 16: Testing
Tensile, hardness, tear, thermal and electrical tests
Tensile Strength (ASTM D412): Measures how far a rubber sample can stretch before it breaks.
Durometer Hardness (ASTM D2240): Checks how hard or soft the rubber is using the Shore A or Shore D scale.
Compression Set: Tests if rubber can bounce back to its original shape after being squeezed for a long time.

## Slide 17: Applications
Tyres, gloves, seals, cables, footwear, medical devices
Rubber is a highly versatile polymer used across various industries due to its elasticity, durability, and waterproofing properties. Major applications include automotive tires, electrical insulation, medical devices (gloves, tubing), footwear soles, and structural shock absorbers. Uncured rubber also serves as a strong adhesive and sealant.
A detailed breakdown of rubber's primary uses includes:
1. Transportation and Automotive
Tires and Tubes: The largest consumer of rubber, utilizing its high elasticity, shock absorption, and abrasion resistance.
Mechanical Components: Used for engine hoses, belts, wiper blades, pedal pads, and vibration-dampening shock mounts.
Seals: Rubber provides airtight and waterproof barriers for vehicle doors, windows, and fuel lines.

## Slide 18
2. Industry and Construction
Seals and Gaskets: Used extensively to prevent fluid, air, and gas leakages in pipelines and machinery.
Belts and Hoses: Utilized for heavy-duty conveyor belts, plumbing, and industrial fluid transportation.
Flooring and Matting: Provides non-slip, shock-absorbing surfaces in commercial spaces, kitchens, and play areas.
Infrastructure: Specialized rubber seismic bearings are placed beneath tall buildings to absorb earthquake shocks.

## Slide 19
3. Healthcare and Safety
Protective Gear: Used in medical, household, and industrial gloves due to its excellent barrier and waterproof properties.
Medical Devices: Essential for syringes, medical tubing, catheters, and orthopedic braces.
4. Everyday Life and Electronics
Electrical Insulation: Because rubber is a poor conductor of electricity, it is used to coat wires, cables, and insulating protective blankets.
Footwear: Provides grip, cushioning, and water resistance in shoes and boots.
Household and Sports: Applied in raincoats, swim caps, elastic bands, pencil erasers, and kitchenware.

## Slide 20: Advantages & Limitations
High elasticity; poor UV/oil resistance
Advantages of Rubber
High Elasticity: Bounces back to original shape after heavy stretching or compression.
Tensile Strength: Resists tearing, cutting, and everyday physical wear.
Waterproof & Airtight: Blocks moisture and gases completely.
Electrical Insulation: Prevents electricity from passing through safely.
Shock Absorption: Dampens vibrations and reduces impact force.
Limitations of Rubber
Poor Oil/Solvent Resistance: Swells and degrades upon contact with gasoline, oils, or harsh chemicals (unless using specialized types like Nitrile Rubber).
UV & Ozone Vulnerability: Cracks and hardens under prolonged sunlight and outdoor weather exposure.
Heat Sensitivity: Standard rubber loses structural integrity at high temperatures.
Aging: Breaks down over time due to environmental oxidation.

## Slide 21: Recent Developments
Recent developments focus on sustainability and advanced performance, include bio-based synthetic polymers derived from renewable biomass like sugarcane, alternative natural rubber sources like guayule, nanotechnology using graphene and silica for stronger nanocomposites, and advanced devulcanization and pyrolysis methods for improved recycling.
Sustainable and Bio-Based Materials
Bio-synthetic polymers: Bridgestone, Michelin, and Goodyear are scaling up plant-derived isoprene and biobutadiene to lower carbon footprints.
Alternative crops: Commercial cultivation of guayule serves as a viable, non-food-crop alternative to traditional rubber trees.
Encapsulation techniques: Spray drying methods are being developed to reduce the stickiness of natural rubber for easier smallholder processing.

## Slide 22
Nanotechnology and Smart Compounds
Nanocomposites: Mixing carbon nanotubes, silica, or graphene into the matrix increases tensile strength and abrasion resistance.
Smart rubber: Embedding sensory micro-elements allows rubber parts to self-monitor stress levels or initiate self-healing mechanisms.
Recycling and Circular Economy
Advanced devulcanization: Breaking sulfur cross-links chemically or via microwaves restores plasticity to waste rubber for high-grade reuse.
Pyrolysis refinement: Thermal breakdown converts end-of-life tires into reusable high-grade carbon black, fuel oil, and synthesis gas

## Slide 23: Environmental Aspects
Recycling, devulcanization, pyrolysis
Rubber has major environmental impacts split between natural rubber farming and synthetic rubber manufacturing. Natural rubber causes deforestation and biodiversity loss in Southeast Asia through large tree monocultures. Synthetic rubber relies on fossil fuels, creates heavy greenhouse gas emissions, and causes chemical pollution.
Natural Rubber Impacts
Deforestation: Clearing tropical rainforests for new tree farms destroys carbon sinks.
Habitat Loss: Monoculture farming reduces local wildlife and plant diversity.
Soil Degradation: Intensive fertilizer and pesticide use harms surrounding land and water.
Synthetic Rubber Impacts
Petrochemical Use: Making synthetic rubber requires large amounts of petroleum and non-renewable energy.
Carbon Footprint: Production plants release high levels of carbon dioxide and hazardous air pollutants.
Chemical Waste: Factory byproducts risk local water and soil contamination. [1, 2]
Disposal and Microplastics
Non-Biodegradable Waste: Tires and discarded goods build up in landfills for decades.
Microplastic Wear: Tire friction on roads sheds rubber particles into air, soil, and waterways

## Slide 24: Types of Synthetic rubber
Synthetic rubber is an artificial elastomer produced via the polymerization of petroleum-based monomers. Tailored for specific industrial, automotive, and commercial needs, the primary types include:
Styrene-Butadiene Rubber (SBR): The most widely produced synthetic rubber. It provides high abrasion resistance and is primarily used for car tire treads, footwear, and adhesives.
Nitrile Rubber (NBR / Buna-N): A copolymer of acrylonitrile and butadiene. It boasts superior resistance to oils, fuels, and chemicals, making it ideal for automotive hoses, seals, and industrial gloves.
Neoprene (Polychloroprene / CR): A versatile rubber known for its exceptional resistance to weathering, ozone, and moderate chemicals. It is used in corrosion-resistant coatings, wetsuits, and gaskets.
Ethylene Propylene Diene Monomer (EPDM): Known for excellent heat, ozone, and weather resistance. It is standard for roofing, steam hoses, and automotive weather stripping.
Butyl Rubber (IIR): Highly impervious to gas and moisture. It is frequently used for medical stoppers, inner tubes, and specialized tire liners.
Silicone Rubber (VMQ / SiR): A rubber offering high-temperature stability and flexibility. It is heavily utilized in medical devices, food-grade surfaces, and electrical insulation.
Fluoroelastomers (FKM / Viton): Engineered to withstand extreme temperatures and harsh chemical environments, often used for aerospace and automotive seals.

## Slide 25: Properties
Synthetic rubbers are man-made elastomers engineered from petroleum hydrocarbons. They offer superior resistance to oils, chemicals, extreme temperatures, and UV weathering compared to natural rubber, making them essential for high-performance automotive, industrial, and consumer applications. [1, 2, 3]
General Mechanical Properties
Elasticity: Stretches under tension and returns to its original shape.
Abrasion Resistance: Withstands heavy friction, rubbing, and surface wear.
Tensile Strength: Varies by compound, offering high load-bearing capacity.
Compression Set: Recovers well after long periods under heavy loads. [1, 2, 3, 4, 5]
Environmental and Chemical Resistances
Weather and UV: Resists ozone, sunlight, and cracking outdoors (especially EPDM).
Chemical Inertness: Resists oils, fuels, and industrial solvents (especially Nitrile and Viton).
Thermal Stability: Maintains flexibility across freezing cold and high heat. [1, 2, 3]
Properties of Common Types
Styrene-Butadiene Rubber (SBR): High wear resistance, low cost; used for tires.
Nitrile Rubber (NBR): Exceptional resistance to oils and fuels.
Neoprene (CR): Balanced resistance to weather, oil, and physical wear.
Silicone: Handles extreme high and low temperatures with medical safety. [1, 2, 3]

## Slide 26
Rubber processing converts raw elastomers into durable goods through mastication, compounding, shaping (extrusion, calendering, molding), and vulcanization. Rubber-fabric composites bond textile reinforcements (nylon, polyester, cotton) with rubber matrices via layering, adhesive dipping, and heat-pressure curing to yield high-strength industrial materials.
Key Rubber Processing Methods
Mastication: Mechanical shearing breaks down high-molecular-weight polymer chains to lower viscosity and soften the rubber.
Compounding: Raw rubber is blended with additives like carbon black, sulfur, plasticizers, and accelerators.
Calendering: The compound passes through rotating heated rollers to generate continuous, precise flat sheets.
Extrusion: The material is forced through specialized dies to form uniform tubes, profiles, or strips.
Molding: Compression, transfer, or injection molding shapes the compound inside a closed cavity.
Vulcanization: Heat and pressure trigger sulfur cross-linking, locking in permanent elasticity and tensile strength. Rubber + Fabric Composite Production Steps
Fabric Preparation: Textiles (such as nylon, aramid, or polyester) are treated with a resorcinol-formaldehyde-latex (RFL) adhesive dip to ensure strong chemical bonding.
Layering & Impregnation: Fabrics and compounded rubber sheets are interleaved or friction-calendered, pressing the elastomer deep into the textile matrix. [1, 2, 3, 4]
Assembly: Multi-ply structures are hand-built or machine-laid up depending on the directional strength required. [1]
Curing (Vulcanization): The composite is placed under high pressure in a press, autoclave, or oven at specific curing temperatures to cross-link the rubber and lock the fabric interface. [1, 2, 3]
Major Rubber-Fabric Composite Products
Pneumatic Tires: Multi-layer textile/steel cord skeletons embedded in rubber.
Conveyor Belts: Fabric-reinforced heavy-duty haulage belts.
Hoses & Tubing: High-pressure braided or wrapped industrial and automotive hoses.
Inflatable Goods: Rubber-coated nylon fabric used for rafts, life vests, and escape slides.
Diaphragms & Gaskets: Fabric-inserted technical membranes for fluid control valves. [1, 2]